Text

Description automatically generated with low confidence

**Product Specification Sheet**

**Part # 21005**

781.767.4511 | [www.EastexProducts.com](http://www.EastexProducts.com)

|  |  |
| --- | --- |
| **Product** | **Tek Stretch 4** |
| **Description** | Tek Stretch 4 is a four-way stretch 100% polyester knit T-jersey laminated with a PU film. |
| **Key Features** | * Fluid Proof * 4-Way Stretch * Cleanable/Wipeable |
| **Applications** | * Medical and Healthcare * Military |
| **Color** | Black |
| **Width** | 54” |
| **Thickness** | .7 mm |
| **Weight** | 240 g/yd |
| **Composition** | Cover Fabric: 100% Polyester Backing: 100% Polyurethane Coating |

| **Test/Property** | **Method** | **Unit/Standard Results** | |
| --- | --- | --- | --- |
| Vapor Permeability: | JIS L1099 B-1 | g/m2/24hr | 500 |
| Water Resistance | JIS L1092-B | mm-H2O | 2000 |