

**Product Specification Sheet**

**Part # 21005**

781.767.4511 | [www.EastexProducts.com](http://www.EastexProducts.com)

|  |  |
| --- | --- |
| **Product**  | **Tek Stretch 4** |
| **Description** | Tek Stretch 4 is a four-way stretch 100% polyester knit T-jersey laminated with a PU film.  |
| **Key Features** | * Fluid Proof
* 4-Way Stretch
* Cleanable/Wipeable
 |
| **Applications**  | * Medical and Healthcare
* Military
 |
| **Color**  | Black |
| **Width** | 54” |
| **Thickness** | .7 mm |
| **Weight** | 240 g/yd |
| **Composition** | Cover Fabric: 100% Polyester Backing: 100% Polyurethane Coating |

| **Test/Property** | **Method** |  **Unit/Standard Results** |
| --- | --- | --- |
| Vapor Permeability:  | JIS L1099 B-1  | g/m2/24hr | 500 |
| Water Resistance | JIS L1092-B  | mm-H2O | 2000 |